Business Opportunity / Technical Need

Industry Need: As semiconductor device dimensions shrink, there is a critical need for low-k (low dielectric constant) spacer materials to reduce parasitic capacitance, improve device speed, and minimize power consumption in advanced logic and memory nodes.

Technical Gap: Conventional silicon-based spacers (e.g., SiN, SiON) have k-values typically above 4.0. BN and BSiN are promising due to their inherently lower k-values, high thermal stability, and potential for improved etch selectivity and integration compatibility.

Market Opportunity: Successful development of BN/BSiN spacers would enable Merck/EMD Electronics to offer next-generation materials for leading-edge semiconductor manufacturing, targeting customers in advanced logic and DRAM.

- Status

Current Focus: The project is actively developing and characterizing BN thin films using ALD (Atomic Layer Deposition) processes. The main precursor under investigation is SN-946, with process variations including TCB/BCl₃ supercycles and NH₃ as a co-reactant.

Experimental Progress: Multiple ALD runs have been completed on the Picosun tool, with systematic variation of process parameters (precursor pulse times, temperatures, supercycle ratios).

Characterization: Extensive ellipsometry (thickness, refractive index), FTIR (bonding environment), and XPS (composition) analyses have been performed. Thickness tracking and in-situ monitoring are ongoing.

Documentation: Results are tracked in MELINDA, with supporting slides and test plans (e.g., "Low K spacer SN-946_Master Summary.pptx", "TRM Debriefing_BN Updates_250827_by PB.pptx").

- Key Learnings

Film Quality: BN films can be deposited with good uniformity and controlled thickness using SN-946 and TCB/BCl₃ supercycles. The process window for optimal film properties is being refined.

Dielectric Properties: Early results indicate promising low-k values, but further optimization is needed to consistently achieve target k < 4.0 while maintaining film integrity.

Process Integration: Supercycle approaches (alternating TCB and BCl₃) influence film composition and properties. NH₃ is critical for achieving desired stoichiometry and minimizing impurities.

Characterization Insights: FTIR and XPS confirm BN bonding environments, but some carbon and oxygen incorporation is observed, which may affect electrical performance.

Tool Reliability: Picosun ALD tool maintenance and seasoning are important for reproducibility.

- Next steps

Process Optimization: Continue refining ALD process parameters (temperature, pulse/purge times, precursor ratios) to further lower k-value and improve film density and purity.

Electrical Testing: Expand electrical characterization (leakage, breakdown, k-value) to benchmark against SiN/SiON and competitive BN solutions.

Integration Studies: Begin integration trials on patterned wafers to assess etch selectivity, thermal stability, and compatibility with downstream processes.

Scale-Up: Prepare for scale-up and technology transfer if target specifications are met, including precursor supply chain and tool matching at customer sites.

Customer Engagement: Share results with key customers and solicit feedback for application-specific requirements.